| Giai đoạn | Phân nhánh các phương án | Điều kiện – Thông số |
| --- | --- | --- |
| #0 – TIỀN XỬ LÝ Xơ dừa → Cellulose | 1. NaOH only | • NaOH 1.5M, 80°C, 2 lần • Yield: 50–60% • Lignin còn: 10–15%→ Cellulose 60–70% |
|  | 2. NaOH + H₂O₂ ⭐ | • NaOH 1.5M + H₂O₂ 10%, 80°C • H₂O₂ 2 lần × 2h • Yield: 40–50% • Lignin còn: <5%→ Cellulose 70–80% |
|  | 3. NaClO₂ | • NaClO₂ 1.7%, pH 4 (acid), 70°C • Yield: 35–45% • Lignin còn: <3%→ Cellulose >80% ⚠️ Tạo dioxin |
| #1 – SOL-GEL & DOPING Cellulose → Hydrogel | 1. Control (không doping) | • Không TEPA, không kim loại • BET ~1000 m²/g • Sensitivity ~50–100 μA/mM/cm² |
|  | 2. N-doping | • 5 mL nước : 4 g Urê : 11 mL (NH4OH25%) • Không kim loại • BET ~1500 m²/g • Sensitivity ~250–350 |
|  | 3. N,S co-doping | • TEPA 1.5–3.0g + Thiourea (12%) • BET ~1800 m²/g • Sensitivity ~400–500 |
|  | 4. Ni doping | • NiCl₂ 0.3–0.6g • TEPA 2.0–3.0g • Sensitivity ~500–650 |
|  | 5. Ni/Co co-doping ⭐ | • NiCl₂:CoCl₂ = 1:2 (mol) • Loading: 15%, 25%, 35% • TEPA scale theo loading • Sensitivity >700 • LOD <0.5 μM |
|  | 6. N,S,Ni/Co ternary ⭐⭐ | • TEPA + Thiourea + NiCo • Sensitivity >850 • LOD <0.3 μM |
| #2 – FREEZE-DRYING Hydrogel → Aerogel | 1. Freeze-drying ⭐ | • H₂O → EtOH → n-Hexane • Đông: −80°C • Thăng hoa: <20 Pa, −40°C, 24–48h • Mesopore: 50–60% • SSA: 1500–2500 m²/g (sau khi KOH ACTIVATION) |
|  | 2. Supercritical CO₂ | • P=74 bar, T=31°C • SSA: 2000–3000 m²/g • Mesopore: 40–50%⚠️ Chi phí cao |
|  | 3. APD | • Sấy 60°C, 3–6h (không chân không) • SSA: 800–1500 m²/g • Co ngót 20–30% |
|  | 4. Vacuum drying | • 60°C, <100 Pa, 12–24h • SSA: 1000–1800 m²/g |
| #3 – KOH ACTIVATION (Optional) Aerogel → Activated Aerogel | Decision gate | • BET #2 SSA >1500 m²/g? YES → SKIP #3NO → Activation |
|  | A. KOH:CA = 0.5:1 | • 750°C, 60’• SSA +300–500 m²/g • Mesopore ~50%✓ An toàn cho NiCo |
|  | B. KOH:CA = 1:1 | • 750°C, 90’• SSA +500–800 m²/g • Mesopore ~40%⚠️ NiCo giảm 10–20% |
|  | SKIP | • Giữ SSA từ #2 • Mesopore 50–60% ✓ Khuyến nghị cho NiCo-doped |
| #4 – CARBONIZATION Aerogel → Carbon Aerogel | 400°C | • N content 8–10% • Conductivity 1–5 S/cm ❌ Không dùng biosensor |
|  | 500°C ⭐ | • N content 5–7% • Conductivity 10–30 S/cm • Pyridinic-N 40–50% |
|  | 550-600°C (Pyrrolic-N) ⭐⭐ | • N content 4–6% • Conductivity 20–50 S/cm • ID/IG ~0.9–1.2 |
|  | 700°C (Pyridinic N) | • N content 2–4% • Conductivity 30–70 S/cm |
|  | 800–900°C (Graphitic N) | • N content <2% • Conductivity >50 S/cm ❌ Không dùng biosensor |
| #5 – ELECTRODE FABRICATION CA → Working Electrode | A. Ni foam ⭐ | • 110 PPI, 1.6 mm • Slurry: CA 80% + Super P 10% + PVDF 10% + NMP • Drop-cast → Sấy 80°C → Ép 10 MPa → Ngâm PBS |
|  | B. GCE | • ∅3–5 mm • Contact area nhỏ, Rct cao hơn |
|  | C. Cu foil / Carbon cloth | • Dày 50–100 μm ⚠️ Cu oxidize trong PBS |
| #6 – ELECTROCHEMICAL TESTING Đo hiệu suất | A. PBS 0.1M pH 7.4 ⭐ | • Test potential: +0.5V vs Ag/AgCl • Sensitivity 700–900 |
|  | B. NaOH 0.1M | • pH ~13 • +0.4–0.5V vs Ag/AgCl ⚠️ Selectivity kém |
|  | Test sequence | • CV → Amperometry → EIS → Selectivity → Stability → Real sample |